BO-OX

RETURN LINE TREATMENT

PREVENTS CORROSION IN STEAM AND CONDENSATE RETURN LINES

FEATURES:

STABLE - Carries to all parts of steam system, even in high-rise buildings and extensive

ground systems with pressure reducing valves.

ECONOMICAL - Liquid treatment vaporizes at boiler water temperatures and recycles

through boiler steam systems.

SAFE - For food plant use.  May be used for corrosion protection in hospital and food

industries where steam comes in direct contact with food, except for milk products.

APPLICATION:

For use in the protection of steam condensate lines.  Neutralizes corrosive carbonic acid

and slowly removes deposits from the system.

DOSAGE:

Use "starting dosage" of 1 pint per 250 gallons of boiler feed water.  Control subsequent

dosages by pH, in the 7.5 to 8.5 range, and/or iron tests performed regularly on the condensate.

The exact dosages should be established in cooperation with your representative.

HANDLING:

BO-OX is an alkaline chemical.  Contact with the body should be avoided.  Avoid

prolonged or repeated breathing of vapor.  Use with adequate ventilation.  In case of skin

contact, wash with plenty of water and soap.  If eyes are affected, flush thoroughly with

water and get medical attention.

FEEDING:

10 ppm maximum when using in steam contacting food, (excluding milk products).  For

maximum economy and optimum control, continuous feed using a positive displacement

chemical metering pump is recommended.  It is not recommended that concentrated BO-OX

be mixed with other concentrated boiler treatments.  BO-OX may be fed to the boiler

feed water line or directly to the boiler or steam line.  Application to the boiler is the preferred

method.

SERVICE:

Regular service calls will be made.  All recommendations and adjustments for correct use will

be discussed with operating personnel at this time.

PACKAGING:

30 gallon drums - 250 lbs. net. & 55 gallon drums - 458 lbs. net.

"WATER TREATING CHEMICALS - WITH SERVICE"

# Text boxes

## Office: 800 - 345 – 7208

www.ryanchemical.com

# P.O. Box 406

Chandler, OK  74834

### RYAN CHEMICAL Co., Inc.