C-239

CLOSED SYSTEM TREATMENT

A NON-CHROMATE CORROSION INHIBITOR

FEATURES:

COMPLETE CORROSION PROTECTION - Protects both ferrous and nonferrous metals.

ANTI-FREEZE - Can be used with anti-freeze solutions.

CONVENIENT AND ECONOMICAL - Ready to use liquid formula can be added directly to the system.

APPLICATION:

C-239 is a highly effective corrosion inhibitor in convenient, ready-to-use, liquid form.  This formula is suitable for use in either hot or chilled water systems, jacket water, & low pressure boilers.

DOSAGE:

INITIAL:  Add 2 gallons of C-239 for each 100 gallons of water in the system to be treated.

CONTINUING:  Subsequent addition of C-239 is governed by the nitrite content of the treated water and depends on the amount of water leakage from the system.  When the sodium nitrite content of the system water drops below 1000 ppm, add 1 gallon of C-239 for each 100 gallons of water in the system.

NOTE:

New installations should be free of oil, grease, and dirt, before charging with C-239.

SERVICE:

Regular service calls will be made by a Ryan representative to make complete water tests at your plant.  All recommendations for correct dosage will be discussed with the operator at this time.

HANDLING:

Does not deteriorate with age.  DO NOT TAKE INTERNALLY.  Avoid excessive exposure of concentrated material to skin.

PACKAGING:

5 gallon pails, 30 gallon drums, & 55 gallon drums.

"WATER TREATING CHEMICALS - WITH SERVICE"

# Text boxes

## Office: 800 - 345 – 7208

www.ryanchemical.com

# P.O. Box 406

Chandler, OK  74834

### RYAN CHEMICAL Co., Inc.