VER-DATE

CLOSED SYSTEM TREATMENT

A NON-CHROMATE CORROSION INHIBITOR

FEATURES:

COMPLETE CORROSION PROTECTION - Protects both ferrous and nonferrous metals.

CONVENIENT AND ECONOMICAL - Ready-to-use liquid formula can be added directly

to the system.

APPLICATION:

VER-DATE is a highly effective Molybdate EDTA corrosion inhibitor in convenient, ready-to-use liquid form.  This formula is suitable for use in either hot or chilled water systems, jacket water, & low pressure boilers.

DOSAGE:

INITIAL:  Add 2 gallons of VER-DATE for each 100 gallons of water in the system to be treated.

CONTINUING:  Subsequent addition of VER-DATE is governed by the content of the treated water and depends on the amount of water leakage from the system.  When the Molybdate content of the system water drops below 10 ppm, add 1 gallon of Ver-Date for each 100 gallons of water in the system.

NOTE:

New installations should be free of oil, grease, and dirt, before charging with VER-DATE.

SERVICE:

Regular service calls will be made by a Ryan representative to make complete water tests at your plant.  All recommendations and adjustments for correct dosage will be discussed with the operator at this time.

HANDLING:

Does not deteriorate with age.  DO NOT TAKE INTERNALLY.  Avoid excessive exposure of concentrated material to skin.

PACKAGING:

30 gallon drums & 55 gallon drums.

"WATER TREATING CHEMICALS - WITH SERVICE"

# Text boxes

## Office: 800 - 345 – 7208

www.ryanchemical.com

# P.O. Box 406

Chandler, OK  74834

### RYAN CHEMICAL Co., Inc.